| #### BREATHER FABRIC | #### AIRBLEED 100 |
| --- | --- |

### DESCRIPTION

Medium weight polyester breather fabric with excellent all round stretch and drapeability.

Effective for use on components having complex curvatures or incorporating acute radii.

Felted construction facilitates efficient resin bleed without risk of bridging and use in single or multiple layers.

### PHYSICAL PROPERTIES

(Maximum Cure Temperature	205C

Fiber					100% Polyester

Color					White or Grey (Please specify)

Weight (nominal)			150 g/m2

Thickness				2.5 mm (nominal, uncompressed)

Note: AIRBLEED 100 has no release characteristics and should be separated from the laminate by a suitable porous release fabric or film. Airbleed 100 is not intended to be used as a breather material alone in high pressure autoclave cures. Data relating to air flow through Airbleed 100 at temperature and pressure is available on request.

### AVAILABILITY & PACKAGING

Standard roll sizes 		100m x 0.76m and 1.52m wideup to 3m wide available to order

Cut shapes 			Available to order

Packaging 	Heavy gauge polyethylene.Wound on 76mm diameter cores

### STORAGE & HANDLING

No special storage conditions required.

No skin irritation problems experienced.

ISSUE DATE OCTOBER 2000

All statements, technical information and recommendations contained in this publication are based on tests believed to be reliable, but their accuracy and/or completeness are not guaranteed. The user shall determine the suitability of the product for this particular purpose and shall assume all risk and liability in connection herewith.

P.O.Box 93            Tel.  +358 9 681 081

FIN 00211           Fax. +358 9 692 4174
HELSINKI