| #### VACUUM BAGGING FILM | #### CAPRAN 77C |
| --- | --- |

### DESCRIPTION

A clear, non-heat stabilised nylon flat cast film.

Predominantly used in de-bulking applications

Very cost effective when compared with the high performance heat stabilised films such as CAPRAN 650 or CAPRAN 518.

### PHYSICAL PROPERTIES

Maximum use temperature		140C short term

Color					Transparent

Tensile Strength			103.4 Mpa

Yield Strength			27.6 Mpa

Elongation				375 - 500%

Tear Strength			20-50g (ASTM D1922)

Shrinkage				2% (0.5hr @ 159C)

Flammability				Self extinguishing melts

Crystalline Melt Point		218 - 220C

### AVAILABILITY & PACKAGING

Thickness (nominal)			0.05mm

Pack size (nominal)			45 kg

Widths				1370 mm, 2134 mm

### STORAGE & HANDLING

All nylon films absorb water.  The higher the moisture content the more flexible they become, conversely at low moisture levels flexibility is reduced.  Capran 77C is despatched with an optimum moisture content to provide maximum performance and handle ability.  To preserve these characteristics during storage the roll should be wrapped in polyethylene and stored at around 65% RH and 20C.

CAPRAN is a tradename of Allied-Signal Inc.

All statements, technical information and recommendations contained in this publication are based on tests believed to be reliable, but their accuracy and/or completeness are not guaranteed. The user shall determine the suitability of the product for this particular purpose and shall assume all risk and liability in connection herewith.

Issue Date: October 2000

P.O.Box 93            Tel.  +358 9 681 081

FIN 00211           Fax. +358 9 692 4174
HELSINKI