| #### SEALANT TAPE | #### SM5144 |
| --- | --- |

### DESCRIPTION

An industry standard in autoclave bonding, composite fabrication and vacuum processing for cure temperatures up to 190OC.

Achieves rapid positive vacuum sealing with most available tool surfaces and bagging materials and allows easy fabrication of pleats, pressure pads and resin dams.

Strips cleanly and quickly from the mould surface on cooling below 66oc.

### PHYSICAL PROPERTIES

Maximum use temperature		90C continuous

205C short term

Color					Yellow, changing to green after cure

Solids				100%

Flammability				Will not support combustion

### AVAILABILITY & PACKAGING

Standard rolls 			9.14 meters long x 12mm x 3mm 
packed in cardboard cartons containing 32 rolls.

### STORAGE & HANDLING

SM5144 is non-toxic, non-irritant, and non-injurious to skin.

Material should be used within 6 months of date of manufacture.

Material must be stored flat.

Cartons should not be stacked more than 5 high.

All statements, technical information and recommendations contained in this publication are based on tests believed to be reliable, but their accuracy and/or completeness are not guaranteed. The user shall determine the suitability of the product for this particular purpose and shall assume all risk and liability in connection herewith.

ISSUE DATE OCTOBER 2000

P.O.Box 93            Tel.  +358 9 681 081

FIN 00211           Fax. +358 9 692 4174
HELSINKI