| #### POLYESTER RESIN | #### SYNOLITE 0529-P-6 |
| --- | --- |

### CHEMICAL/PHYSICAL NATURE

Synolite 0529-P-6 is a low viscous, pre- accelerated, promoted, thixotropic, medium reactive unsaturated polyester resin based on orthophthalic acid. An LSE system has been incorporated.

### MAJOR APPLICATIONS

Synolite 0529-P-6 is recommended for high performance constructional laminating.

### PRINCIPAL PROPERTIES

Synolite 0529-P-6 combines good mechanical properties with optimal processability. This resin shows very good fibre wetting and impregnation properties. Due to the thixotropic properties the resin does not sag on vertical surfaces. Full retention of lap shear strength after delayed lay-up can be reached if the surface is not too resin rich.

### PRODUCT SPECIFICATIONS

Property			Range			Unit		TM

Appearance 			Hazy			-		2265

Acid value, as such  		11 - 17			mg KOH/g	2401

Viscosity, Brookfield RVT, 
2 rpm, 23°C 			700 – 1000		mPa.s		2313

Viscosity, Brookfield RVT, 
20 rpm, 23°C 		290 – 390		mPa.s		2313

Viscosity, Brookfield RVT, 
250 rpm, 23°C 		210 - 230		mPa.s		2313

Solids content, IR 		56 - 58			%		2033

Gel time from 25 to 35°C 	22 - 27			minutes	2625

Cure time from 25°C 
to peak 			35 – 45		minutes	2625

Peak temperature 		120 - 150		°C		2625

Remarks

Viscosity measurement:

TM 2313: Brookfield RVT, 2/ 20/ 250 rpm, 23°C.

TM2625: 2.0 g Butanox M-50 in 100 g resin.

### PROPERTIES OF THE LIQUID RESIN (TYPICAL VALUES)

Property			Value			Unit		TM

Colour on sight  		pink/green		-		-

Density, 23°C		appr. 1100		kg/m³		2160

Flash point 			appr. 33		°C		2800

Stability, no init, 
dark, 25°C			6			months	-

### PROPERTIES OF CAST UNFILLED RESIN (TYPICAL VALUES)

Property			Value			Unit		TM

Tensile strength 		78			MPa		ISO 527-2

Tensile E-modulus 		3.4			GPa		ISO 527-2

Elongation at break 		3.2			%		ISO 527-2

Flexural strength 		135			MPa		ISO 178

Heat Deflection 
Temp. (HDT) 		80			°C		ISO 75-A

Impact res. - unnotched sp. 	11			kJ/m²		ISO 179

Hardness 			50-55			Barcol		2604

Density, 23°C		±1200			kg/m³		-

Volume shrinkage 		7.5			%		-

Curing conditions

Cured with 2% Butanox M-50. Postcured 24 hrs RT followed by 24 hrs 60°C and 24 hrs 80°C.

### PROPERTIES OF GLASS REINFORCED RESIN (TYPICAL VALUES)

Property			Value			Unit		TM

Glass content 		± 30			%		-

Tensile strength 		125			MPa		ISO 527-2

Tensile E-modulus 		8.2			GPa		ISO 527-2

Flexural strength 		205			MPa		ISO 178

Curing conditions

Cured with 2% Butanox M-50 and postcured 24 hrs RT followed by 24 hrs 60°C and 24 hrs 80°C.

### GUIDELINES BEFORE USE

Before use, the resin should be conditioned at a well defined, application dependant temperature (usually 15°C minimum for a MEKP / Co cure). Stir the product before use.

### STORAGE GUIDLINES

The resin should be stored at a dark and dry place at temperatures between 5°C and 30°C. Shelf life is reduced at higher temperatures. The shelf life of styrene containing unsaturated polyesters will be significantly reduced when exposed to light. Store in dark and in 100% light tight containers only.

### MATERIAL SAFETY

A material safety data sheet for the product is available on request.

### TEST METHODS

Test methods (TM) referred to in the table(s) are available on request.

Although the facts and suggestions in this publication are based on our own  research and are  believed reliable, we cannot assume any responsibility for performance or results obtained through the use of our products herein described, nor do we accept any liability for loss or damages directly or indirectly caused by our products. The user is held to check the quality, safety and all other properties of our product prior to use. Nothing herein is to be taken as permission, inducement or recommendation to practise any patented invention without a license.

Version: 002623/2.0 Date of issue: October 2000

P.O.Box 93            Tel.  +358 9 681 081

FIN 00211           Fax. +358 9 692 4174
HELSINKI